**20.02.2019**

**FS No.40**

|  |  |
| --- | --- |
| Article Description | Metallised Embroidery Thread |
| Composition | 40% metallised polyester; 35% polyamid; 25% paper |
| Count | dtex 220 / den 200 |
| Make Up Available  | 1000m spool ; 5000m cone |

|  |  |
| --- | --- |
| **Fastness Rating – Scale 1 (worst) – 5 (best)** |  |
| Fastness to washing at 60°C DIN EN ISO 105-C03/M & S C4A | 4-5 |
| Fastness to water (damp for 4hrs at 37°C) DIN EN ISO 105-E01/M & S C6 |  4-5 |
| Fastness to rubbing dry (10 rubs on dry white Fabric) DIN EN ISO 105-X12/M & S C8 | 4 |
| Fastness to rubbing wet (10 rubs on wet white Fabric) DIN EN ISO 105-X12/M & S C8 |  3-4 |
| Fastness to dry cleaning DIN EN ISO 105-D01 |  4-5 |
|  |  |
| **Fastness Rating – Scale 1 (worst) – 8 (best)** |  |
| Fastness to light (100hrs xenon light) DIN EN ISO 105-B02  | 5-6 |
| Due to different dye stuffs not applicable to all colors. |  |
|  |  |
| **Mechanical – Technological Values** |  |
| Tensile Strength cN (force until thread breaks, in Centinewton) DIN EN ISO 2062 | ca. 500 |
| Elongation (% of stretch extension with weight tension until breaks) |  ca.40 |
|  |  |
| **Special note:**Please note that colors 4001, 4002, 4003, 4005, 4006, 4007, 4008, 4010, 4021, 4022, 4026, 4071 might oxidize. All other colors of the FS 40 range are resistant to oxidation. |
| **Recommendations for care** |  |
| M:\Dokumente und Einstellungen\iso101\Lokale Einstellungen\Temporary Internet Files\Content.Outlook\A14R0P31\Waschen_60_Grad.jpg Dreieck_NICHT_BLEICHEN M:\Dokumente und Einstellungen\lab202\Lokale Einstellungen\Temporary Internet Files\Content.Word\Trocknersymbol_1Punkt.jpg M:\Dokumente und Einstellungen\iso101\Lokale Einstellungen\Temporary Internet Files\Content.Outlook\A14R0P31\Bügeln_1_Punkt.jpg M:\Dokumente und Einstellungen\lab202\Lokale Einstellungen\Temporary Internet Files\Content.Word\Textilpflege_chemisch.jpg  |  |
|  |  |
| **Color Card No.** | **63** |
|  |  |
| **Öko-Tex:**  C:\Users\lab202\AppData\Local\Microsoft\Windows\INetCache\Content.Word\OTS100_label_95.0.4921_en.jpg  |  |